| TECTYL 210-R This information only applies to products manufactured in the following location(s): Europe Description TECTYL 210 R is an amber colored, solvent cutback, wax base, thixotropic corrosion preventive compound. TECTYL 210 R is designed for protection at factory level of enclosed boxes, seams, joints and other creviced locations of vehicles, susceptible to corrosion. TECTYL 210 R cures to a semi-hard, waxy, light amber colored, translucent slightly tacky film. ___________________________________________________________________________ Typical Properties Flashpoint; PMCC 40 °C Specific Gravity @ 60°F 0.86 kg/ltr Recommended Dry Film Thickness 50 microns minimum Theoretical Coverage @ Avg. Recommended DFT 7.5 m²/l Non Volatile 44 weight % Viscosity; DIN (53 211) Cup No. 4 @ 20°C 25 seconds (at time of manufacture) Cure Time @ 25°C ± 24 hours Volatile Organic Content (VOC) (ASTM D-3960) 478 g/l Accelerated Corrosion Tests: @ Avg. Recommended DFT Salt Spray; 5 % NaCl @ 35°C; DIN 50 021 (ASTM B-117) 21+ days (DIN 1623 Steel Panels) Humidity; 100 % RH; @ 40°C; DIN 50 017-KK 100+ days (DIN 1623 Steel Panels) | Tectyl 210-R Эта информация относится только к продукции, произведенной в следующие места (мест): Европа Описание Tectyl 210 г янтарного цвета, растворителя сокращение, воск базы, тиксотропные Антикоррозионные соединения. Tectyl 210 R предназначен для защиты на заводе уровень закрытых коробках, швов, стыков и других трещиноватый местах транспортных средств, подвержены коррозии. Tectyl 210 R исцеления полутвердые, восковые, свет янтарного цвета, прозрачный слегка липкой пленки. ___________________________________________________________________________ Типичные свойства Flashpoint; PMCC 40 ° C Удельный вес при 60 ° F 0,86 кг / л Рекомендуемая толщина сухой пленки 50 микрон минимальной Теоретический расход @ Ср. Рекомендуемой толщине 7,5 м ² / л Энергонезависимой 44% по весу Вязкость, DIN (53 211) Кубок № 4 при 20 ° C 25 секунд (В процессе изготовления) Время отверждения при 25 ° C ± 24 часов Содержание летучих органических (ЛОС) (ASTM D-3960) 478 г / л Ускоренное коррозионных испытаний: @ Ср. Рекомендуемой толщине Солт Спрей; 5% NaCl при 35 ° С; DIN 50 021 (ASTM B-117) 21 + дней (DIN 1623 стальных панелей) Влажность, 100% RH, при 40 ° С, DIN 50 017-KK 100 + дней (DIN 1623 стальных панелей) |
| --- | --- |

| Surface Preparation: The maximum performance of TECTYL 210 R can be achieved only when the metal surfaces to be protected are clean, dry and free of rust, oil and mill scale. Valvoline recommends that the metal substrate temperature be 10-35 °C at the time of product application. Application: TECTYL 210 R is formulated to be used as supplied. Ensure uniform consistency prior to use. Continued stirring is generally not required. If the product thickens due to cold storage or loss of solvent during use, contact Valvoline. DO NOT THIN TECTYL 210 R. Incorrect thinning will affect film build, dry time and product performance. Valvoline recommends that the ambient and product temperature be 10-35 °C at the time of product application. TECTYL 210 R can be applied by airless or airmixing spray. Removal: TECTYL 210 R can be removed with mineral spirits or any similar petroleum solvent, hot alkaline wash or low pressure steam. Storage: TECTYL 210 R should be stored at temperatures between 10-35 °C. Mild agitation is recommended prior to use. Due to its composition TECTYL 210 R can be subject to postproduction viscosity changes during storage. Under proper storage conditions TECTYL 210 R can have a shelf life of 3 years minimum. Caution: Adequate ventilation is required for cure and to ensure against formation of combustible liquid. THE PARTIALLY CURED FILM SHOULD NOT BE EXPOSED TO IGNITION SOURCES SUCH AS FLARES, FLAMES, SPARKS, EXCESSIVE HEAT OR TORCHES. Refer to Valvoline’s Material Safety Data Sheet for additional handling and first aid information. Note: The addition of any product over or under this coating is not recommended. The use of additional coatings could result in chemical incompatibility, thus affecting the performance of this coating as stated in the Typical Properties section. If a primer, other than a Valvoline recommended product is required, written authorization must be obtained from Valvoline. | Подготовка поверхности: Максимальную производительность Tectyl 210 R может быть достигнуто только тогда, когда металлические поверхности на защиту являются чистыми, сухими и свободными от ржавчины, масла и окалины. Valvoline рекомендует температуры металлической подложки быть 10-35 ° C на время применения продукта. Применение: Tectyl 210 R разработан для использования при поставке. Убедитесь однородной консистенции перед использованием. Продолжение шевелясь, как правило, не требуется. Если продукт утолщается за счет холодного хранения или потери растворителя в процессе использования, обратитесь Valvoline. НЕ ТОНКИХ Tectyl 210 Р. Неправильный истончение повлияет на толщину пленки, время высыхания и производительность продукта. Valvoline рекомендует окружающей среды и температуры продукта быть 10-35 ° C на время применения продукта. Tectyl 210 R можно наносить безвоздушным или airmixing брызг. Удаление: Tectyl 210 R могут быть удалены с уайт-спиритом или любого аналогичного нефтяного растворителя, горячая мыть щелочным или пар низкого давления. Хранение: Tectyl 210 R должны храниться при температуре от 10-35 ° C. Мягкий агитации рекомендуется перед использованием. Благодаря своему составу Tectyl 210 R может быть предметом постпродакшн изменения вязкости во время хранения. При надлежащих условиях хранения Tectyl 210 R может иметь срок хранения 3 года минимум. Внимание: Адекватная вентиляция, необходимых для лечения, и обеспечить, чтобы предотвратить образование горючей жидкостью. Частично отвержденный фильм не должен подвергаться источников воспламенения, как вспышки, огонь, искры, чрезмерного тепла или факелами. Обратитесь к Valvoline в Паспорт безопасности для дополнительной обработки и первая информация помощь. Примечание: Помимо какого-либо продукта или под этим покрытием не рекомендуется.Использование дополнительных покрытий может привести к химической несовместимости, что отражается на производительности это покрытие, как указано в разделе Типичные Свойства. Если грунтовка, кроме Valvoline рекомендовано производить работы, письменное разрешение должно быть получено от Valvoline. |
| --- | --- |