Description

TECTYL ML  -Spray- is a wax based, solvent cutback, amber colored corrosion preventive compound which is supplied in an aerosol spray can.

TECTYL ML  -Spray- has good water displacing properties and good penetration, making it very suitable as a corrosion protective for the inside of car doors and other hollow sections of cars and rolling equipment.

TECTYL ML  -Spray- cures to an amber colored, waxy, semi-firm translucent film.

Typical Properties

Nature of propellant:	Propane/Butane.

Flashpoint; PMCC:	< 0	°C

Recommended Dry Film Thickness	50	microns

Accelerated Corrosion Tests:

@ Avg. Recommended DFT

Salt Spray; 5 % NaCl @ 35°C; DIN 50 021 (ASTM B-117)	21+	days

(DIN 1623 Steel Panels)

Humidity; 100 % RH; @ 40°C; DIN 50 017-KK	75+	days

(DIN 1623 Steel Panels)

Surface Preparation:

The maximum performance of TECTYL ML  -Spray- can be achieved only when the metal surfaces to be protected are clean, dry and free of rust, oil and mill scale. Valvoline recommends that the metal substrate temperature be 10-35 °C at the time of product application.

Application:

TECTYL ML  -Spray- gives a maximum performance when it is sprayed at an ambient and product temperature of 10-25 °C. Shake the can with TECTYL ML  -Spray- well before use and spray at a distance of approximately 25 cm from the surface.

As the TECTYL ML  -Spray- is a fast drying product this can cause “pin-holing” when the product is applied too thick at once. Valvoline advises to spray one layer per pass, wait for 2 to 3 minutes and then spray another layer. Continue like this until the required film thickness has been obtained.

DO NOT FREEZE TECTYL ML  -Spray-.

Removal:

TECTYL ML  -Spray- can be removed with mineral spirits or any similar petroleum solvent, hot alkaline wash or low pressure steam.

Storage:

TECTYL ML  -Spray- should be stored at temperatures between 10-35 °C. Shaking the can well prior to use is recommended. For storage after use invert the can and spray for a few seconds to clear the nozzle. The container is pressurized. Keep away from flammable substances and protect from direct sunlight and temperatures over 50°C.

Caution:

Adequate ventilation is required for cure and to ensure against formation of combustible liquid. THE PARTIALLY CURED FILM SHOULD NOT BE EXPOSED TO IGNITION SOURCES SUCH AS FLARES, FLAMES, SPARKS, EXCESSIVE HEAT OR TORCHES. Refer to Valvoline’s Material Safety Data Sheet for additional handling and first aid information.